## Slide 1: Hydrodeoxygenation of fast pyrolysis oil over Pd/Al2O3 catalyst
VIMAL KUMAR, Department of Chemical Engineering , IIT Roorkee, India
B. Prasad, Department of Chemical Engineering, IIT Roorkee, India
D. V. Naik, M.O. Garg, CSIR-Indian Institute of Petroleum, Dehradun, India
Lovraj Kumar Memorial Trust (LKMT) R&D Meet
July 24–25, 2015: IIChE NRC, New Delhi

## Slide 2: Outline of the presentation
Introduction
Hydrodeoxygenation of FPO?
Experimental setup
Results and discussion
Conclusions

## Slide 3: Worldwide energy scenario
The worldwide consumption of liquid fuels is bound to increase from 87 to 97 million barrels per day from 2010 to 2020, respectively and it is projected to 115 million barrels per day in 2040 [John et al. 2013]
Source: Shell energy scenario to 2050 (shell international BV, 2008)
Notes: EJ= Exajoules=1.0E+18

## Slide 4: India’s national policy on bio-fuels
First generation bio-fuels
  A target of 20% blending of biofuels, both for bio-diesel and bio-ethanol, by 2017 is proposed.
Second generation bio-fuels
  Not yet proposed
Source: http://mnre.gov.in/file-manager/UserFiles/biofuel_policy.pdf
Notes: EJ= Exajoules=1.0E+18

## Slide 5: General Budget 2015-16
The Ministry of New and Renewable Energy has revised its target of renewable energy capacity to 1,75,000 MW till 2022, comprising
  1,00,000 MW Solar,
  60,000 MW Wind,
  10,000 MW Biomass and
  5,000 MW Small Hydro
Source: http://pib.nic.in/budget2015/budgetdoc/gbEngRelease.pdf
Notes: EJ= Exajoules=1.0E+18

## Slide 6: Second generation biofuels
The conversion of lignocellulosic biomass into hydrocarbons addresses
Clean energy
Sustainability
Environment issues

## Slide 7: Pyrolysis techniques
Techniques | Residence Time | Heating Rate | Temp (°C) | Products
Carbonization | Days | Very Low | 400 | Charcoal
Conventional | 5-30 min | Low | 600 | Oil, gas, char
Fast | 0.5-5 sec | Very High | 650 | Bio-oil
Flash-liquid | <1 sec | High | <650 | Bio-oil
Flash-gas | <1 sec | High | <650 | Chemicals, gas
Ultra | <0.5 | Very High | 1000 | Chemicals, gas
Vacuum | 2-30 sec | Medium | 400 | Bio-oil
Hydro-pyrolysis | <10 sec | High | <500 | Bio-oil
Methano-pyrolysis | <10 sec | High | >700 | Chemicals

## Slide 8: Fast pyrolysis reactors development status
Reactor | Technology | Owned by | Capacity, TPD* | Construction, Year | Application
Auger | ABRI-Tech | ABRI-Tech | 50.0 | 2008 | Energy
Ablative | BTO® | Pytec, Germany | 6.0 | 2005 | CHP#
Bubbling fluid bed | BioThermTM | Dynamotive, Canada | 200 | 2007 | Energy
Circulating fluid bed | Ensyn/RTPTM | Ensyn, Canada | 75 | 2007 | CHP#
Rotating cone | BTG-BTL | Empyro BV, Netherlands | 120 | 2012 | CHP#
*TPD: Tons per day #CHP: Combined heat and power |  |  |  |  | 

## Slide 9: Fast pyrolysis
“Rapid thermal decomposition of organic material in an oxygen-free environment”
Operating principles
  Short residence time < 2 sec
  Higher heating rate > 1000 ºC/s
  Moderate temperature 400-550ºC
  Moisture content <10%
  Quick separation of char particles
  Rapid quenching of pyrolysis vapors
Salient Features
  Higher conversion ~ 85-90%
  Maximum liquid yield ~ 60-75 wt.%
  Qualitative bio-char yield ~ 10-15 wt.%

## Slide 10: Fast pyrolysis reactors development status [Venderbosch et al. 2010]
Reactor | Technology | Owned by | Capacity, TPD* | Construction, Year | Application
Auger | ABRI-Tech | ABRI-Tech | 50.0 | 2008 | Energy
Ablative | BTO® | Pytec, Germany | 6.0 | 2005 | CHP#
Bubbling fluid bed | BioThermTM | Dynamotive, Canada | 200 | 2007 | Energy
Circulating fluid bed | Ensyn/RTPTM | Ensyn, Canada | 75 | 2007 | CHP#
Rotating cone | BTG-BTL | Empyro BV, Netherlands | 120 | 2012 | CHP#
*TPD: Tons per day #CHP: Combined heat and power |  |  |  |  | 

## Slide 11
Fast pyrolysis oil properties, challenges
Fast pyrolysis oil properties
Not miscible with fossil hydrocarbons
Not distillable
Highly oxygenated (H/Ceff < 0.5)
Highly corrosive (pH: 2 - 4)
High water content (15-35 wt.%)
Lower heating value (16-19 MJ/kg)
Fast pyrolysis oil challenges
Unstable due to ageing (polymerization of oxy compounds)
Competitive pricing to fossil hydrocarbons

## Slide 12: Effective Hydrogen-to-Carbon Ratio

## Slide 13: Modification of chemical composition
In-process (gas phase)
Catalytic pyrolysis
  Catalytic-mixing
  Catalytic bed
  Co-catalytic
Process parameters
  Rector configuration
  Temperature
  Pressure
  Environment
  Layout
Post-process (liquid phase)
Thermal treatment
Hydrothermal treatment
High pressure thermal treatment
Catalytic emulsion
Catalytic hydrogenation
Techniques for stabilization of FPO

## Slide 14: Fast pyrolysis unit
Salient features:
Capacity: 3 kg/h
Reactor: Bubbling fluidized bed
Heating media: Sand
Biomass: Jatopha expelled cake (particle size: 1.4 mm)
Temperature: 530 °C
Pressure: 1 atmosphere
FPO unit at IIP Dehradun

## Slide 15: Autoclave reactor: Hydrodeoxygenation of FPO
Salient features:
Capacity: 600 ml
Feed: Crude pyrolysis oil
Catalyst: Pd/Al2O3 catalysts
Reactor: CSTR (Batch)
Temperature: 250-300 °C
Pressure: 80 bar

## Slide 16: Catalyst Preparation
Palladium (99.9%, Sigma-Aldrich Chemicals) and γ-alumina Al2O3 (97%, Sigma-Aldrich Chemicals) were chosen as an active and support materials for the preparation of hydrodeoxygenating catalyst.
Mesoporous alumina was prepared using incipient wetness impregnation method.
  The Pd was loaded over alumina.
  1.0 g of Palladium (II) nitrate dihydrate was dissolved in 30 ml of water, and 20 ml of ethanol and 20 g of γ-alumina (Al2O3) (Surface area = 243 m2 g-1) was added simultaneously.
  The mixture was stirred constantly at 80 °C for 5 hours to dry the sample.
  The dried sample was further dried at 120 °C for overnight in an oven. Finally, the Pd metal loaded on alumina was calcined at 500 °C in a furnace for 8 h to prepare Pd/Al2O3 catalyst (2% Pd on alumina).

## Slide 17: Hydrodeoxygenation of FPO
A 100 ml stainless steel, high pressure stirred tank reactor (M/s Autoclave Engineers, USA) with bolted closure, floor stand and magnetic drive assembly was used to partially hydrodeoxygenate the heavy fraction of FPO in batch mode.
Before starting the reaction, the reactor was purged with hydrogen gas for a period of 5 min, and then it was pressurized up to 80 bar pressure.
A constant speed of stirrer was maintained at 700 rpm.
The reactor temperature was raised to 250 0C/300 0C from ambient with heating rate of 5 0C min-1.
As a result an increase in reactor pressure was observed from 80 to 120 bars.
The same temperature was maintained for a period of 4 h.
The reactor was then cooled down to ambient temperature.
The liquid products were collected and analyzed separately using NMR spectroscopy.

## Slide 18: Elemental analysis: Biomass Feedstock, FPO and HDO
Sample name | C, wt.% | H, wt.% | N, wt.% | O, wt.% | S, wt.% | H/C | O/C
Jatropha curcas cake | 45.50 | 6.70 | 2.43 | 45.33 | 0.04 | 1.76 | 0.74
Fast pyrolysis oil | 56.50 | 7.10 | 4.30 | 32.0 | 0.09 | 1.50 | 0.42
HDO oil at 250 °C | 64.98 | 8.0 | 4.91 | 22.0 | 0.11 | 1.50 | 0.25
HDO oil at 300 °C | 76.18 | 8.8 | 4.91 | 10.0 | 0.11 | 1.40 | 0.09

## Slide 19: Van Krevelen Diagram: Biomass Feedstock, FPO and HDO oils

## Slide 20: 31P NMR Characterization of (a) FPO; (b) HDO at 250 °C; and (c) HDO at 300 °C

## Slide 21: (a) 1H NMR of HDO at 300 °C, (b) 1H NMR of HDO at 250 °C, (c) 1H NMR of FPO, (d) 13C NMR of HDO at 300 °C, (e) 13C NMR of HDO at 250 °C, (f) 13C NMR of FPO

## Slide 22
Sr. No. | Functional group | Integration region, ppm |  | FPO | HDO oil, 250 °C | HDO oil, 300 °C
 |  | Ben et al. 2013 | Present study |  |  | 
1 | Aliphatic OH | 150.0 to 145.5 | 150.02 to 145.07 | 2.37 | 0.27 | Nil
2 | C5 substituted β-5 | 144.7 to 142.8 | 145.07 to 140.42 | 1.23 | 0.6 | Nil
3 | Guaiacyl phenolic OH | 140.0 to 139.0 | 140.42 to 138.2 | 6.2 | 1.51 | Nil
4 | p-hydroxy-phenyl OH | 138.2 to 137.3 | 138.2 to 136.96 | 5.75 | 1.89 | Nil
Hydroxyl Group Contents of FPO and HDO Determined by quantitative 31P NMR
Derivatization with 2-chloro-4, 4, 5, 5-tetramethyl-1, 3, 2-dioxaphospholane (TMDP)

## Slide 23: A selectivity data for co-processing of FPO and HDO with VGO
Feedstock’s | VGO:FPO |  |  |  | VGO:HDO | VGO | VGO:FPO
Blending ratio | 95:5 | 90:10 | 85:15 | 80:20 | 95:5 | 100 | 83:17
FCC conversion, % | 75.68 | 74.69 | 69.35 | 64.39 | 66.96 | 66.89 | 66.08
Yield, wt.% |  |  |  |  |  |  | 
Dry gas (C1-C2) , wt.% | 2.182 | 2.05 | 1.43 | 1.41 | 1.507 | 1.798 | 1.42
LPG (C3-C4), wt.% | 38.876 | 35.70 | 28.69 | 23.77 | 28.78 | 15.5 | 25.44
Gasoline (C5-216°C), wt.% | 29.038 | 31.14 | 35.11 | 35.04 | 32.50 | 44.02 | 35.08
LCO (216-370°C), wt.% | 14.885 | 15.43 | 17.99 | 20.49 | 18.98 | 19.84 | 19.11
HCO(>370°C), wt.% | 8.054 | 8.48 | 10.67 | 14.08 | 13.27 | 12.4 | 12.31
Coke, wt.% | 5.48 | 5.21 | 4.23 | 4.16 | 4.17 | 5.58 | 4.14
[Naik et al., RSC Advances, 5, 398-409, 2015]

## Slide 24: Conclusions
Hydroxyl and mono lignol groups were eliminated during hydrodeoxygenation.
HDO oil obtained at 300 °C can be used along with VGO as a co-processing feedstock for processing in a refinery FCC unit.
The trillion dollars of petroleum refinery infrastructure and their existing distribution network can be effectively utilized.

## Slide 25: Acknowledgements
All co-authors
Special thanks to Indian Institute of Technology Roorkee and
CSIR-Indian Institute of Petroleum for their technical and
financial support.

## Slide 26
Thank you very much for your kind attention

## Slide 27: Reaction scheme for derivatized 31P NMR

## Slide 28: Catalyst Characterization
N2 adsorption-desorption isotherm
XRD patterns of the mesoporous alumina (black colour) and Pd supported on mesoporous alumina (red colour)

## Slide 29: Catalyst Characterization: SEM monograms
Mesoporous alumina
Pd supported mesoporous alumina

## Slide 30: Bubbling fluidized bed reactor
Features:
Heat supplied externally to bed
Good heat & mass transfer
Easy scale up
Well understood technology
Small particle size needed (< 2mm)
Heat transfer to bed at large scale has to be proven

## Slide 31: Dynamotive energy systems
Process Scheme
4 T/hr Demonstration Plant